## Slide 1: Recent Progress in Advanced Materials and Instrumentation Tests at the MIT Reactor
Lin-wen Hu*, Gordon Kohse, David Carpenter
*Director, Research and Services

## Slide 2: MIT Nuclear Reactor Laboratory
MIT-NRL is an interdepartmental laboratory with missions in nuclear technology applications, neutron science research, and training/education.
Primary facility is MIT Reactor (MITR), a multi-purpose research reactor owned and operated by MIT. A partner facility of DOE’s Nuclear Science User Facilities (NSUF).
Constructed in 1958 (MITR-I), upgraded in 1975 (MITR-II) with new core tank and housing
Uprated from 5 MW to 6 MWth in 2010 (2nd largest university reactor in US).
Compact core with power density similar to a LWR. Operates 24/7, 10-week cycles
Tank-type, light water cooled and moderated, D2O and graphite reflector.
Excellent track record in in-pile irradiation experiments including LWR loop, fuel, high-temperature materials, and advanced instrumentations.

## Slide 3: MITR Cross-Section

## Slide 4: Neutron Flux and Spectrum
Facility | Size | Neutron Flux (n/cm2-s)
In-core | 3 available Max in-core volume ~ 1.8” ID x 24” long | Thermal: 3.6x1013 Fast: up to 1.2x1014 (E>0.1 MeV)
Beam ports | Various radial: 4” to 12” ID | Thermal: 1x1010 - 1x1013 (source)
Vertical irradiation position | 2 vertical (3GV) 3” ID x 24” long | Thermal: 4x1012 - 1x1013
Through ports | One 4” port (4TH) One 6” port (6TH). | Avg thermal: 2.5x1012 to 5.5x1012
Pneumatic Tubes | One 1” ID tube* (1PH1) | Thermal: up to 8x1012
 | One 2” ID tube* (2PH1) | Thermal: up to 5x1013
Fission Converter Beam Facility (FCB) | Beam aperture ~ 6” ID | Epithermal: ~ 5x109
Thermal Beam Facility (TNB) | Beam aperture ~ 6” ID | Thermal: up to 1x1010
Fast flux is ~ 20% of ATR

## Slide 5
Since 2006, NRL research and services division has grown to 13 staff (10 PhDs)
Expanding Research Group

## Slide 6: NRL Research
neutrons
Focus
New sensors
  Fiber-optics
  Crack-length
  Ultrasonic
New materials
  Fuels (UZrH, metallic)
  Ceramics (SiC, carbon fiber, MAX-phase)
  Metals (zirconium, 3D-printed steels)
  Coolants (liquid flibe salt, lead bismuth)
Neutron optics
  Neutron lenses
  Radiography

## Slide 7: In-Core Materials Irradiation
3 in-core positions dedicated to experiments
General facilities for specimen capsules
  PWR/BWR conditions in water loop
  Inert gas up to 850°C
Customized facilities for high temperatures (>1300°C) and exotic materials (e.g. fluoride salts, fissile materials up to 100 gm U-235)
Common measurements: corrosion, swelling, property changes, activation, radiolysis
Materials in Extreme Environments
Accident tolerant cladding
Advanced fuels
Liquid salts
Very high temperatures

## Slide 8: Recent In-Core Experiments
ACI
SiC LWR cladding in PWR conditions
BSiC
SiC channel box and guide tubes
WATF
Accident-tolerant cladding and coatings
ICCGM
Actively-loaded real-time crack growth monitor
COATI
ATF SiC coated plates and tubes with ECP
Pressurized Water Loop
Fuel Tests
HYFI
U-Zr-H LWR fuel rods with liquid metal bonding
AFTR
Internally- and Externally-Cooled Annular Fuel
FS-1
FHR coupons in flibe at 700°C and tritium capture
FS-2
Additional coupons, salt, and activation sampling
FS-3
FHR and SINAP ceramics, guard heating
Fluoride Salt
HTIF
Ceramics and TRISO >1400
Drexel
MAX-phase materials at 300-700°C in inert gas
LUNA
Fiber optics at 700°C
ULTRA
Ultrasonic transducer and self-powered detector test
ULTRA 2
Ultrasonic and fiber optic sensors at 800°C
HYCO
ATF SiC coated plates and tubes at 320°C
TREAT
Neutron and gamma transient benchmark
Inert Gas

## Slide 9: Radiation-Hardened Ultrasonic Sensors
Collaboration with INL and Pennsylvania State University,
  Six different ultrasonic transducers
  Real-time response as a function of flux, temperature, fluence
Miniaturized neutron and gamma detectors also successfully tested
Follow-up collaboration with INL, CEA, University of Pittsburgh, and AFO Research
  Includes optical glasses and radiation-hardened fiber optics

## Slide 10: In-Core Crack Growth Monitors
Collaboration with INL to adapt an in-core crack growth measurement technique from the Halden Reactor Project (Norway).
  Crack growth is actively controlled, and the crack length measured in real-time
Successful demonstration provides a path forward to deployment in US test reactors.
  High-pressure miniature bellows development (3000 psi in-core)
  Establishing new test protocols
  Observation and mitigation of significant radiation-induced signal noise (including new saturation phenomena)
MITR operating flexibility key to achieving desired test evolution

## Slide 11: LWR In-Core Electrochemical Potential
COATI contains 3 ECP probes
  Real-time measurement of the electrical potential between a passive electrode and the structure of the loop
Probes are located near the core to capture the local corrosion environment (radiolysis)
Experimental probes able to withstand high temperature, pressure, PWR chemistry

## Slide 12: Ongoing Contributions to Accident Tolerant Fuel Development
The MITR water loop is one of the primary irradiation test beds for SiC/SiCf, hybrid (composite on metal alloy) and coated clad materials and sealing techniques
  Many of these materials have been exposed to irradiation in prototypical coolants for the first time
PWR or BWR conditions with a wide range of B/Li and dissolved gas concentrations , zinc injection, 16N suppression additives
Collaboration with Westinghouse, CTP, General Atomics, and Oak Ridge National Laboratory, as well as MIT NSED faculty and staff (Mike Short, Ju Li, Koroush Shirvan)

## Slide 13: HYCO – Hybrid Composites
Collaboration with Oak Ridge National Laboratory for Accident Tolerant Fuel materials development
60 metal and ceramic specimens irradiated at 320°C in the ICSA (helium)
Undergoing PIE in NRL hot cells prior to shipment to ORNL

## Slide 14: COATI
CTP and ORNL Accident Tolerant Clad Irradiation
New silicon carbide metal-coated materials at 290°C and 1500 psi in the water loop
Follow-on to HYCO ICSA irradiation of similar materials

## Slide 15: First-of its-Kind Molten Salt Irradiations Completed at MIT
2 fluoride redox potentials
Added graphite and C/C coupons
Tritium and salt interaction with fuel compact graphite
Cracking performance of TRISO particles
300 hours at 700°C
First in-core irradiation of MSRE flibe in 60 years
1000 hours at 700°C
TRISO, Hastelloy, SS316, and SiC corrosion specimens
Flibe is 99.995% 7Li; still substantial tritium release
FS-1
FS-2

## Slide 16: Fluoride Salt Irradiation #3 (FS-3)
Large matrix of graphite and C/C specimens (95)
Applying lessons learned
  More fluoride capture options/protect instrumentation
  Electrical guard heating
  Hydrogen injection system
MSRE enriched flibe cleaned at UW-Madison, analyzed at MIT via NAA
Flibe and specimens loaded into graphite crucibles at UW
Dried in furnace at MIT, then assembled into nickel capsule under helium

## Slide 17: Fluoride Salt Tritium Permeation (FS-4)
Use MITR thermal neutron beam (3GV) to continuously generate tritium in flibe salt at 600-700C
  Vertical position for improved access, flux
  Electrical heating complemented with nuclear
Investigate steady-state tritium diffusion through metals, barrier coatings
  Salt contact on inside surface
Thermal neutrons
45 cm tall
~1x1013 n/cm2-s

## Slide 18
External tube furnace allows tritium diffusion testing in the absence of neutron or gamma irradiation
Quartz barrier prevents tritium release at high temperature
Multiple test sections can be quickly installed
  Bare 316SS
  Alumina coated (with intermediate coatings) 316SS
Three days of operation at low power
  100-200kW with natural flibe produces sufficient tritium
  620°C flibe temperature
  He/H2 purge gas in four independent flow systems
Order of magnitude reduction in tritium permeation with “first-effort” alumina coating
Fluoride Salt Tritium Permeation (FS-4)

## Slide 19: TREAT – INL Transient Test Reactor
A graphite-moderated, graphite-reflected, air-cooled reactor
  Steady-state operation up to 100 kW
  Pulsed operation up to 18,000 MW
Fueled with 93.1% enriched UO2 particles finely dispersed in graphite
TREAT core has maximum of 361 fuel assemblies (19 x 19)

## Slide 20: TREAT Instrumentation Tests
Collaboration with Oregon State University, University of Michigan, and INL on instrumentation and benchmarking in support of the TREAT restart
Irradiations in the MITR test sensors and produce data to support code benchmarking
  TREAT steady-state equivalent <100 kW
  Positive and negative reactivity insertion transients
Follow-on irradiation with identical setup in TREAT (M8CAL test position)
MPFD
Fission wire
  Natural uranium, U/Cd
Activation wires/foils
  Al-Co, Fe, Fe-Ni-Cr, Nb, Ti, Cu-Au
Self-Powered Detectors
  Gamma (platinum), Neutron (vanadium)
Miniature Fission Chambers
  Enriched uranium in metal rods
Micro-Pocket Fission Detectors
  Uranium and thorium in a metal rod
Mini FC
First university-led experiment completed in June 2018.

## Slide 21: Shipment to INL-TREAT
Irradiated Experiment Test Assembly (from MIT to INL)
Irradiated Activation Wires (from TREAT to INL Counting Lab)

## Slide 22: Installations
Loading Instrumentation Assembly into TREAT M8CAL Core
Experiment Top View
Arranging Cables
Complete Shielding

## Slide 23: TREAT Experiment

## Slide 24
Beam ports/neutron radiography
Pneumatic tubes/rabbits
Neutron activation analysis - High-efficiency gamma spectroscopy and scintillation lab
Hot cell and hot box facilities
  Optical profilometry - 1.6µm x 12nm resolution
  Scanning electron microscopy with EDS
  Xenon-flash thermal diffusivity analyzer
  New PIE lab in restricted area (SEM, instron machine etc. )
Supporting and PIE Capabilities

## Slide 25: Summary
MITR offers complementary capability to DOE test reactors (ATR, TREAT, HFIR) and plays an important role in national programs such as Nuclear Science User Facilities (NSUF), Accident Tolerant Fuel, advanced sensors/instrumentations.
MIT-NRL research team is specialized in new reactor experiment demonstration such as crack growth monitor, and high-temperature salt and materials irradiation to support FHR/MSR program.
Demand has increased from DOE programs (through NEUP/NSUF/GAIN programs, national labs) and industry (TerraPower, KairosPower, Westinghouse)
  Advanced reactors, materials and sensors development program
  MITR’s ease-of-access to university and industry researchers
  Track-record in project execution.

## Slide 26
Thank you!